## Slide 1
The Solid State Chemistry
“The universe consists only of atoms and the void: all else is opinion and illusion.”–Edward Robert Harrison

## Slide 3
Conventional & Primitive Unit Cells
Unıt Cell Types
Primitive
A single lattice point per cell
The smallest area in 2 dimensions, or
The smallest volume in 3 dimensions
Simple Cubic (SC)
Conventional Cell = Primitive cell
More than one lattice point per cell
Volume (area) = integer multiple of
that for primitive cell
Conventional
(Non-primitive)
Body Centered Cubic (BCC)
Conventional Cell ≠ Primitive cell

## Slide 5
Extra distance =
BC + CD =
2d sinq
= nl
(Bragg Equation)

## Slide 6: Summing the waves
The overall scattering intensity depends on
Atom types (as above) - “electron density”
Their position relative to one another.
Or for simple (centrosymmetric) structures:
This is the sum of the (cos) waves, where:
- fj is the atomic scattering factor for atom j
- hkl are the Miller indices
- xj, yj, zj are the atomic (fractional) coordinates
Centrosymmetric means that there is a “centre of symmetry”, and for every atom at (x,y,z) there is an identical atom at (-x, -y, -z)

## Slide 7
The expression 2(hx+ky+lz) =  phase difference or phase factor
Where F(hkl) is the structure factor for the hkl reflection of the unit cell, f is the atomic scattering factor for each of j atomic planes and  is the repeat distance between atomic planes measured from a common origin (called the phase factor)
Scattering by an unit cell = f(position of the atoms, atomic scattering factors)
For n atoms in the UC
Structure factor is independent of the shape and size of the unit cell! F → Fhkl

## Slide 8
Structure factor calculations
A
Atom at (0,0,0) and equivalent positions
 F is independent of the scattering plane (h k l)
Simple Cubic
 All reflections are present
Note:
n is an integer
Some useful relations
Now we perform calculation of structure factor calculations for some simple crystal structure unit cells.
We basically perform the summation of the function fexp(i) for the different atoms ions in the unit cell and work out the restrictions on the allowed values of hkl (and the corresponding intensities).
We note that in simple cubic crystals there is no restrictions on the allowed values of hkl (i.e. for all values of hkl reflections are present).
a
UC in reciprocal space
1/a

## Slide 9
B
Atoms at (0,0,0) & (½, ½, 0) and equivalent positions
 F is independent of the ‘l’ index
C- centred Orthorhombic
Real
Both even or both odd
Mixture of odd and even
e.g. (001), (110), (112); (021), (022), (023)
e.g. (100), (101), (102); (031), (032), (033)
(h + k) even
(h + k) odd
For this case there is one additional lattice point with an associated atom. Hence, there will be two terms in the summation for the structure factor.
UC in reciprocal space
1/a
1/b
1/c
Important note:
The 100, 101, 210, etc. points in the reciprocal lattice exist (as the corresponding real lattice planes exist), however the intensity decorating these points is zero.